Macintosh Restorations

Cleanse Your Item

- Use compressed air to remove any hard-to-reach dirt and or dust on or in your item.

- Use soap and water to carefully lather the plastic, making sure to go over any scuffs or dirt that may be in crevices.

- Go over with a towel to dry.

Gather Your Restoration Materials

- Your Item

- Hydrogen Peroxide 3%

- Xanthan Gum

- Glycerin USP

- Oxy-Pro Multi-Purpose Stain Remover

Mixing Your Materials

- Grab a Medium Sized Bucket

- Pour the entire bottle of Peroxide in the bucket.

- Start stirring your peroxide mix and slowly add 1 TBSP of Xanthan Gum until filly mixed.

- Add 2 TBSP of Glycerin into your mixture then blend until fully mixed.

- Add ¼ TBSP of Oxy-Pro into your mixture and mix thoroughly.

Restore Your Macintosh

- Make sure that your yellowed plastics have been separated from the electronics within your item.

- Lay out your item(s) in a neat, secluded area.

- Grab a brush/sponge and evenly spread your restoration mixture on the yellowed parts of your item.

- (Summer) After spreading out the mixture on your item evenly, lay it out in the sun for approximately 2-3 hours without any wind interference.

- (Winter) Lay under a UV lamp for 2-3 days.